典型干式加工

机架

材料:	St37K	(DIN 174 FL 50x40) 加工设备:	TRAUB TNA 300

速度:	50－	5,000 rpm

冷却润滑剂 :

以前 (wet):	乳化液

现在 (MQL)	准干式润滑剂

湿加工	干式加工

切削速度

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

1st  setup

1st  setup

| 车刀 | 180 | 0,18 | External turning tool | 200 | 0,20 |
| --- | --- | --- | --- | --- | --- |
| 麻花钻 Ø 19 | 60 | 0,10 | Twist drill Ø 19 | 200 | 0,06 |
| 车刀 | 200 | 0,10 | External turning tool | 220 | 0,10 |
| 镗刀 | 150 | 0,08 | Internal turning tool | 180 | 0,10 |
| 攻丝刀 | 65 | 1,50 | Threading tool | 100 | 1,50 |
| 内开槽刀具 | 60 | 0,06 | Internal recessing | 130 | 0,08 |
|  |  |  | tool |  |  |

合计时间:	3’06	min

Total time: 1’57 min

Time saved:  37 %

准干式加工典型应用

盖板

Material:	GG 20	RD40

Machine:	Heckert BAZ CWK400D Speed range:	50	15,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed speed

Cutting speed

Feed speed

Tools

VC  [m/min]

V  [mm/min]	Tools

VC  [m/min]

Vf [mm/min]

| Step drill | 100 | 588 | Solid carbide step | 73 | 61 |
| --- | --- | --- | --- | --- | --- |
| Ø 12.5 Ø 15 |  |  | drill Ø 5.8 Ø 10; Fire |  |  |
| Counterbore | 50 | 90 | Solid carbide step | 73 | 441 |
| Ø 5.8 Ø10 |  |  | drill Ø 5.8; Fire |  |  |
| Solid carbide drill | 100 | 327 | Solid carbide step | 73 | 505 |
| Ø 5.8 |  |  | drill Ø 4.6; Fire |  |  |
| Solid carbide drill | 100 | 270 | Solid carbide step drill | 73 | 505 |
| Ø 4.5 |  |  | Ø 4.8. Ø 12.5; Fire |  |  |
| Solid carbide drill | 100 | 260 | Solid carbide step drill | 73 | 517 |
| Ø 4.6 |  |  | Ø 4.5; Fire |  |  |
| Solid carbide drill | 100 | 270 | Tap M14x1.5 TiN | 30 | 1023 |
| Ø 4.8 |  |  |  |  |  |
| Solid carbide drill | 100 | 328 | Solid carbide step | 73 | 441 |
| Ø 5.8 |  |  | drill Ø 5.8; Fire |  |  |
| Solid carbide drill | 100 | 549 | Solid carbide reamer | 8,4 | 54 |
| Ø 12.5 |  |  | Ø 6 G7 TiAlN |  |  |
| Tap M14x1.5; HSS | 15 | 1024 | Countersink Ø 6.5 | 73 | 447 |
| HSS drill Ø 12.3 | 100 | 463 |  |  |  |

Ø 6 drilled out to G7 tolerance on special machine

Total time:	5’24 min

Total time:	1’48 min

Time saved:  67 %

准干式加工典型应用

垫板

Material:	GG 20	RD40

Machine:	Heckert BAZ CWK400D Speed range:	50	15,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed speed

Cutting speed

Feed speed

Tools

VC  [m/min]

V  [mm/min]	Tools

VC  [m/min]

Vf [mm/min]

| SC drill Ø 3.2 | 80 | 145 | SC step drill | 73 | 598 |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Ø 2.8, Fire |  |  |
| Drill Ø 2.5 | 35 | 28 | SC reamer | 18 | 210 |
|  |  |  | Ø 3 H7 TiAlN |  |  |
| Tap M3 TiAlN | 30 | 142 | SC step drill | 70 | 562 |
|  |  |  | Ø 2.5, Fire |  |  |
| Drill Ø 2.7 | 35 | 30 | SC countersink Ø 3,4 | 73 | 684 |
|  |  |  | SC step drill | 73 | 581 |
|  |  |  | Ø3.2, Fire |  |  |
|  |  |  | End mill Ø 3 | 110 | 47 |

Ø 3 drilled out to H7 tolerance on special machine

Tap M3 TiN

SC step drill

Ø 3.4, Fire

30

126

1592

1888

Total time:	3’12 min

Total time:	1’30 min

Time saved:  53 %

准干式加工典型应用

机架

Material:	16MnCr5 1.7131  (DIN 1017 FL40x30) Machine:	Heckert BAZ CWK400D

Speed range:	50	15,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed speed

Cutting speed

Feed speed

Tools

VC  [m/min]

V  [mm/min]	Tools

VC  [m/min]

Vf [mm/min]

| NC spotting drill Ø 10 | 70 | 80 | NC spotting drill Ø 10 | 80 | 250 |
| --- | --- | --- | --- | --- | --- |
| SC twist drill Ø 4 | 63 | 100 | SC twist drill Ø 4 | 90 | 760 |
| SC twist drill Ø 9,8 | 77 | 450 | SC twist drill Ø 9,8 | 77 | 860 |
| Countersink for core | 24 | 30 | Countersink for core | 47 | 250 |
| M14x1,5 |  |  | M14x1,5 |  |  |
| Countersink for core | 20 | 80 | Countersink for core | 46 | 280 |
| M12x1,5 |  |  | M12x1,5 |  |  |
| Step drill | 43 | 30 | Step drill | 72 | 180 |
| Ø 23 / Ø 12,5 |  |  | ø 23 / ø 12,5 |  |  |
| SC twist drill Ø 9,0 | 80 | 450 | SC twist drill Ø 9,0 | 80 | 665 |
| Countersink for core | 23 | 25 | Countersink for core | 70 | 300 |
| M12x1,0 |  |  | M12x1,0 |  |  |
| Countersink Ø 6/30° | 8 | 40 | Countersink ø 6/30° | 38 | 225 |
| Tap M12x1 | 11 | 300 | Thread miller | 87 | 200 |
|  |  |  | M12x1.5; pitch 1 |  |  |
| Tap M14x1,5 | 19 | 300 | Thread miller | 87 | 240 |
|  |  |  | M14x1.5; pitch 2 |  |  |
| Tap M12x1,5 | 17 | 300 | Thread miller | 87 | 240 |
|  |  |  | M12x1.5; pitch 2 |  |  |

Production on 3 machine tools	Production on a machining center

made possible by the use of MQL tools

Total time: 15’42 min

Total time: 6’36 min

Time saved:  58 %

准干式加工典型应用

联接法兰盘

| Material: | X10 CrNiS 18 9 1.4305 | (DIN 668 RD30) |
| --- | --- | --- |
| Machine: | TRAUB TNA 300 |  |

Speed range:	50	5,000 rqm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed fn  [mm/rev]

Cutting speed

Feed fn  [mm/rev]

Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

| Turning tool | 220 | 0,20 | Turning Ø 28 | 250 | 0,25 |
| --- | --- | --- | --- | --- | --- |
| Twist drill Ø 19 | 15 | 0,14 | Disposable drill Ø 19 | 160 | 0,06 |
| Centering drill | 19 | 0,12 | Drilling Ø 8.7 | 60 | 0,08 |
| Twist drill Ø 8 | 10 | 0,12 | Drilling Ø 10 | 60 | 0,08 |
| Flat drill Ø 18 | 34 | 0,10 | Internal turning | 250 | 0,10 |
| Flat drill Ø 10 | 13 | 0,12 | Thread chasing | 90 | 1,50 |
|  |  |  | M22x1.5 |  |  |
| Internal turning tool | 152 | 0,12 | Groove milling | 38 | 400 |
| Internal turning tool | 207 | 0,08 |  |  |  |
| Thread | 55 | 1,50 |  |  |  |
| Recess | 50 | 0,06 |  |  |  |
| Groove milling | 19 | 70,00 |  |  |  |

Fewer machining operations

thanks to modified tools

Total time:	5’00 min

Total time:	2’04 min

Time saved:  59 %

准干式加工典型应用

盘件

Material:	AlCuMgPbF38  (DIN 1770 Fl 80x15) Machine:	TRAUB TNA 300

Speed range:	50	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

1st  setup

1st  setup

| T Max drill Ø 25 | 64 | 0,12 | T Max drill Ø 24 | 200 | 0,25 |
| --- | --- | --- | --- | --- | --- |
| External rough turning | 440 | 0,15 | External rough turning | 800 | 0,25 |
| External finish turning | 485 | 0,08 | External finish turning | 855 | 0,25 |
| Internal turning Ø 26H7 | 90 | 0,08 | Internal turning Ø 26H7 | 300 | 0,25 |
| Chamfer 1x45° | 71 | 0,04 | Chamfer 1x45° | 200 | 0,15 |

Total time:	2’45 min

Total time:	0’45 min

Time saved:  73 %

准干式加工典型应用

泵主轴

Material:	X35CrMo17 1.4122	(DIN 1013 RD 22) Machine:	new: Brother TC 227

Speed range:	0	10,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

c	f	c	f

Time saved:  70 %

准干式加工典型应用

阀体

Material:	9SMnPb28K	(DIN 174 Fl 40x25) Machine:	TRAUB TNA 300

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	           准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed fn  [mm/rev]

Tools

VC  [m/min]

f   [mm/rev]	Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

1st  setup

1st  setup

| Predrilling | 50 | 0,20 | Facing | 280 | 0,25 |
| --- | --- | --- | --- | --- | --- |
| Predrilling | 50 | 0,20 | T Max drill Ø 19 | 170 | 0,20 |
| Facing | 470 | 0,08 | Undercut | 150 | 0,12 |
| Rough turning | 120 | 0,06 | Fit Ø 20H9 turned | 200 | 0,10 |
| Inside diameter |  |  | Thread M22x1,5 |  |  |
| turning | 120 | 0,06 | milled | 4000 min 1 | 500 |
| Thread cutting |  |  |  |  |  |
| M22x1,5 | 10 | 1,50 |  |  |  |

Total time:	3’18 min

Total time:	1’48 min

Time saved:  45 %

准干式加工典型应用

法兰块

| Material: | Al Mg Cu Pb | F38 |
| --- | --- | --- |
| Machine: | DMG Twin 65 |  |

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed fn  [mm/rev]

Cutting speed

Feed fn  [mm/rev]

Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

| Roughing | 250 | 0,30 | Facing, roughing | 275 | 0,20 |
| --- | --- | --- | --- | --- | --- |
| Rough drilling | 50 | 0,12 | Rough drilling | 125 | 0,20 |
| External finishing | 230 | 0,10 | Centering (2x) | 225 | 300 |
| Drilling (2x) | 32 | 120 | Drilling Ø 2,4 (2x) | 105 | 280 |
| Tapping M3 (2x) | 5 | 0,50 | Centering (2x)/ | 180 220 | 950 |
|  |  |  | deburring |  |  |
| Internal finishing | 95 | 0,08 | Drilling Ø 4.8 (2x) | 180 | 250 |
| Recessing | 47 | 0,05 | External finishing | 275 | 0,15 |
|  |  |  | Tapping M3 (2x) | 4 | 0,50 |

2nd setup

Internal finishing	95

0,15

|  |  |  | Ø 12 E9 |  |  |
| --- | --- | --- | --- | --- | --- |
| Rough countersinking | 60 | 0,10 | Recessing | 50 | 0,10 |
| Boring | 165 | 0,05 | Facing, chamfering | 345 | 0,15 |
| Centering (7x) | 70 | 125 | Centering, deburring | 160 220 | 980 |
| Drilling Ø4.8 (2x) | 53 | 175 | Milling | 135 | 540 |
| Drilling Ø2H9 (2x) | 25 | 120 | Counterboring Ø 8 | 250 | 250 |
| Drilling Ø2.5 (5x) | 32 | 120 | Drilling Ø 2.4 (5x) | 90 | 240 |
| Tapping M3 (5x) | 3 | 0,50 | Tapping M3 (5x) | 4 | 0,50 |
| Counterboring | 50 | 80 | Drilling Ø 2H9 (2x) | 100 | 300 |
|  |  |  | Rough countersinking | 50 | 0,15 |
|  |  |  | Ø 24 |  |  |

Completed in 2 setups of blanks.

Boring

Parting

200

120

0,12

0,12

Total time:	8’5 min

Total time:	3,7 min

Time saved:  56,5 %

准干式加工典型应用

导向杆

Material:	AlCuMgPb F38  (DIN 1798 RD14) Machine:	TRAUB TNA 300

Speed range:	0－	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

1st  setup

1st  setup

| Threads | 150 | 1,25 | Threads | 400 | 0,08 |
| --- | --- | --- | --- | --- | --- |
|  | 2nd setup |  |  | 2nd setup |  |
| Centering | 57 | 0,10 | Centering | 180 | 0,12 |
| Drilling Ø 4.0 | 31 | 0,10 | Drilling Ø 4.0 | 180 | 0,12 |
| Turning | 97 | 0,10 | Turning | 200 | 0,12 |
| Thread chasing | 67 | 8 strokes | Thread chasing | 90 | 8 strokes |
| M14x1.5 thread |  |  | M14x1.5 thread |  |  |
| Deburring | 97 | 0,12 | Deburring | 200 | 0,12 |

Total time:	4’21 min

Total time:	2’08 min

Time saved:  49 %

准干式加工典型应用

活塞

Material:	AlMgSi1  (DIN 1798 RD 40) Machine:	TRAUB TNA 300

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

External turning tool

Centering drill

1st  setup

150

7,5

0,10

0,08

External turning tool

Centering drill

1st  setup

150

7,5

0,10

0,08

| External turning tool | 315 | 0,25 | External turning tool | 475 | 0,25 |
| --- | --- | --- | --- | --- | --- |
| External turning tool | 345 | 0,12 | External turning tool | 540 | 0,15 |
| Ext. recessing tool | 150 | 0,08 | Ext. recessing tool | 240 | 0,30 |
| Ext. recessing tool | 150 | 0,08 | Ext. recessing tool | 225 | 0,20 |
| Ext. recessing tool | 220 | 0,10 | Ext. recessing tool | 260 | 0,08 |
| Ext. recessing tool | 150 | 0,10 | Ext. recessing tool | 400 | 0,03 |
| Twist drill Ø 4,0 | 15 | 0,08 | Twist drill Ø 4.0 | 15 | 0,08 |
| Twist drill Ø 2,5 | 10 | 0,08 | Twist drill Ø 2.5 | 10 | 0,08 |

Tap M3

External turning tool

Centering drill

1,5

2nd  setup

315

11,5

0,50

0,12

0,10

Tap M3

External turning tool

Centering drill

1,5

2nd  setup

315

11,5

0,50

0,12

0,10

Total time:	3’17 min

Total time:	2’30 min

Time saved:  24 %

准干式加工典型应用

Flange AZ7 0108MGEFLA 001

Material:	AlCuMgPbF38  (DIN 1799 RD120) Machine:	TRAUB TNA 300

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

Twist drill  Ø 17	60

0,15

Disposable drill Ø 17

283

0,25

| External turning tool | 750 | 0,25 | External rough turning | 600 | 0,30 |
| --- | --- | --- | --- | --- | --- |
| Internal turning tool | 160 | 0,20 | Shaping pass | 260 | 0,30 |
| Face recessing | 120 | 0,08 | Internal finish turning | 280 | 0,06 |
| External turning tool | 565 | 0,20 | External finish turning | 650 | 0,22 |
| External turning tool | 565 | 0,12 |  |  |  |
| Internal turning tool | 125 | 0,12 |  |  |  |

Fewer machining operations due to modified tools

Total time:	4’52 min

Total time:	0’53 min

Time saved: 	82 %

准干式加工典型应用

工作活塞

Material:	16 Mn Cr 5

Machine:	DMG Twin 65

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed fn  [mm/rev]

Cutting speed

Feed fn  [mm/rev]

Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

Tools

VC  [m/min]

Feed speed

Vf  [mm/min]

Facing / roughing

Rough milling

70

120

0,18

100

Roughing

Facing

160

200

0,30

0,12

| Milling | 45 | 80 | Boring | 135 | 0,05 |
| --- | --- | --- | --- | --- | --- |
| Profile milling | 30 | 80 | Tap M6x0.5L | 15 | 0,50 |

Deburring

Parting

40	400

65	0,10

Milling

Profile milling

Milling

Finish milling Radius cutting Deburring Finishing Centering Recessing Rough milling Finish turning

115

120

100

125

100

95

90

20

92

95

250

900

720

480

750

400

1000

0,23

0,03

0,10

380

0,10

Total time:	6’00 min

Total time:	3’50 min

Time saved: 	41,7 %

准干式加工典型应用

连接法兰

Material:	AlMgSiPb F28  (DIN 1796 4Kt 50) Machine:	TRAUB TNA 300

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

|  | 1st setup |  |  | 1st setup |  |
| --- | --- | --- | --- | --- | --- |
| External turning tool | 210 | 0,12 | External turning tool | 300 | 0,20 |
| Disposable drill | 113 | 0,15 | Disposable drill | 165 | 0,06 |
| External turning tool | 230 | 0,10 | External turning tool | 315 | 0,10 |
| Internal turning tool | 205 | 0,12 | Internal turning tool | 235 | 0,10 |
| Threading tool | 49 | 2,30 | Threading tool | 140 | 1,50 |
| Internal turning tool | 205 | 0,15 | Internal turning tool | 235 | 0,08 |

Total time:	2’48 min

Total time:	1’28 min

Time saved: 	48 %

准干式加工典型应用

Material:	AlMgSi0,5F22  (DIN 1799 RD55) Machine:	TRAUB TNA 300

Speed range:	0	5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

| Facing + rough turning | 450 | 0,40 | Facing + rough turning | 420 | 0,40 |
| --- | --- | --- | --- | --- | --- |
| Disposable drill Ø 30 | 47 | 0,12 | Disposable drill Ø 30 | 365 | 0,25 |
| Flat drilling Ø 38 | 77 | 0,15 | Flat drilling Ø 38 | 350 | 0,20 |
| Inside turning tool | 200 | 0,30 | Inside turning tool | 375 | 0,15 |
| Recessing tool | 42 | 0,05 | Hollowing Ø 40H8 | 600 | 0,06 |
| Inside turning tool | 80 | 0,10 | Inside turning tool | 105 | 0,05 |
| Hollowing Ø 40H8 | 125 | 0,08 | Hollowing | 450 | 0,40 |
| Smoothing | 150 | 0,15 | Outside turning tool | 520 | 0,15 |
| Outside turning tool | 350 | 0,12 |  |  |  |

Total time:	7’46 min

Total time:	1’42 min

Time saved:  78 %

准干式加工典型应用

定位环

Material:	AlMgSiPbF28  (DIN 1796 4KT50) Machine:	TRAUB TNA 300

Speed range:	0－5,000 rpm

Cooling lubricant

原来 (wet):	乳化液

现在(MQL)	准干式润滑剂

Wet machining	Dry machining

Cutting speed

Feed

Cutting speed

Feed

Tools

VC  [m/min]

f   [mm/rev]	Tools

VC  [m/min]

fn  [mm/rev]

|  | 1st setup |  |  | 1st setup |  |
| --- | --- | --- | --- | --- | --- |
| Centering drill | 15 | 0,20 | Centering drill | 15 | 0,20 |
| External turning tool | 240 | 0,25 | External turning tool | 300 | 0,40 |
| Disposable drill Ø 30 | 110 | 0,15 | Disposable drill Ø 30 | 165 | 0,22 |
| External turning tool | 250 | 0,15 | External turning tool | 315 | 0,25 |
| Internal turning tool | 205 | 0,12 | Internal turning tool | 235 | 0,25 |
| Internal recessing tool | 57 | 0,10 | Internal recessing tool | 75 | 2,30 |
| Internal threading tool | 75 | 2,30 | Internal threading tool | 140 | 2,30 |
| Internal turning tool | 205 | 0,15 | Internal turning tool | 235 | 0,20 |

Total time:	2’30 min

Total time:	1’22 min

Time saved: 	45 %

准干式加工典型应用

法兰

材料:	AlCuMgPbF38  (DIN 1799 RD120)

设备:	Traub TNA 400德国特劳伯数控车床

速度:	0－5,000 rpm

冷却润滑剂:

原来 (wet)	乳化液

现在 (MQL)	准干式润滑剂

Wet Machining	Dry Machining

Cutting speed

Feed

Cutting speed

Feed

Tools

Vc  [m/min]

f   [mm/rev]	Tools

Vc  [m/min]

fn  [mm/rev]

|  | 1st setup |  |  | 2nd setup |  |
| --- | --- | --- | --- | --- | --- |
| T Max drill Ø 17 | 290 | 0,25 | External turning tool | 600 | 0,35 |
| External turning tool | 600 | 0,35 | External turning Ø 70j6 | 110 | 0,10 |
| Face recessing | 260 | 0,30 | External turning tool | 650 | 0,15 |
| Internal turning tool | 345 | 0,12 |  |  |  |
| External turning tool | 150 | 0,08 |  |  |  |

Total time:	0’54 min

Total time:	0’21 min

Time saved:  61 %

# Text boxes

n

f

f

f

n

| Wet machining | Dry machining |
| --- | --- |
| Cutting speed Feed speed Tools V [m/min] V [mm/min] | Cutting speed Feed speed Tools V [m/min] V [mm/min] |
| Solid carbide miller 18,8 30 | Solid carbide miller 65 207 Ø 3, coated |
| Deburring manual | Miller Ø 3 50 742 |
| Universal milling machine |  |
| Total time: 1’39 min | Total time: 0’30 min |

n

n

| Centering | 5 | 0,10 | Centering | 20 | 0,20 |
| --- | --- | --- | --- | --- | --- |
| Finishing Ø 12 f8 | 83 | 0,10 | Finishing Ø 12 f8 | 180 | 0,06 |
| Deburring Ø 3 | 30 | 0,10 | Deburring Ø 3 | 60 | 0,10 |
| Drill Ø 6.8 | 12 | 0,10 | Drill Ø 6.8 | 60 | 0,10 |
| Drill Ø 9 | 15 | 0,10 | Drill Ø 9 | 40 | 1,50 |

n

n

| Finishing | 80 | 0,10 | Centering | 12 | 0,05 |
| --- | --- | --- | --- | --- | --- |
| Recessing | 95 | 0,10 | Drilling Ø6.2/5.5 | 40 | 0,07 |

n

|  | 2nd setup |  |  | 2nd setup |  |
| --- | --- | --- | --- | --- | --- |
| External turning tool | 220 | 0,08 | External turning tool | 300 | 0,08 |
| Internal turning tool | 265 | 1,50 | Internal turning tool | 265 | 1,50 |
| Internal recessing | 75 | 0,06 | Internal recessing | 75 | 0,06 |

n

n

|  | 2nd setup |  |  | 2nd setup |  |
| --- | --- | --- | --- | --- | --- |
| External turning tool | 240 | 0,20 | External turning tool | 300 | 0,25 |
| Internal turning tool | 205 | 0,12 | Internal turning tool | 235 | 0,20 |

n